## Slide 1: Synthesis and Characterization of Environmentally Benign Cu/PVA Nanocomposites
Kim Lykens, Stebbins High School
Todd Hamilton, Academy of World Languages
Faculty Mentors: Dr. George Sorial &
Dr. Margaret Kupferle
Graduate Research Assistant: Ayenachew Tegenaw
Grant #EEC-1404766
Notes: Both

## Slide 2
Abstract
Introduction
Literature Review
Goals & Objectives
Research Design (Methods, Training, Results)
VI. Research Conclusions
VII. Unit Topics
Table of Contents
Notes: Kim

## Slide 3
Abstract
Copper/polyvinyl alcohol (Cu/PVA) nanocomposites were synthesized using chemical reduction method
Characterized by various microscopy and spectroscopy techniques
Stability analysis under various environmental conditions
Rate of catalytic degradation for methylene blue pollutant
http://sustainable-nano.com/2013/07/17/nanoparticles-with-your-coffee-a-java-infused-science-experiment/
Nanoparticle
Notes: Kim
Atoms, molecules, or clusters (Chemical reducation method)

## Slide 4
Introduction
http://www.wichlab.com/research/
Nanoparticles:
Between 1-100nm in size at least in one dimension
Notes: Kim

## Slide 5
Introduction (cont.)
Nanoparticles:
                High surface-area-to-volume ratio
Unique physical/chemical properties
Novel applications
Concerns:
Environmental toxicity (hydrosphere, lithosphere, atmosphere, biosphere)
Ethical concern
Copper (Cu) Nanoparticles:
Biocide, catalyst, antimicrobial
Economical and abundant
http://people.forestry.oregonstate.edu
Notes: Kim catalytic behavior
Production of Chemical Weapons

## Slide 6
Synthesis Approach (Top-Down & Bottom-Up):
Pieces of metal are milled into smaller particles
Chemically synthesizing nanoparticles (Borm et al., 2006)
Synthesizing Nanoparticles:
Electrolyte salt and Cu precursor
Stabilizing/capping agent (Ramesh et al., 2012)
Stabilization Mechanisms
Electrostatic
Steric
Electrosteric (Fritz et al., 2002)
Polyvinyl alcohol (PVA):
Stabilizing agent
Non-toxic, biodegradable, water-solubale (Patachia, 2003)
Literature Review
https://en.wikipedia.org/wiki/Colloid
Notes: Kim
Agglomeration influences the:
Size of nanoparticles
Physicochemical properties (Borm et al., 2006)

## Slide 7
Goal:
Synthesize environmentally benign Cu/PVA nanocomposites
Objectives:
Synthesis and characterization
Assessing impact of environmental factors (pH, ionic strength, electrolyte valence, humic acid) on particle size
Degradation of organic pollutant under UV light
Goal and Objectives
Notes: Kim
Monovalent (NaCl)– one charge +1
Divalent (CaCl2)—two charge +2
Ionic strength= intensity of ions (concentration)

## Slide 8
Research Design
  Analytical Design
  Synthesis
  -Carbonate
  -Iodine
  -Hydroxide
Notes: Todd

## Slide 9
Nanoparticle Synthesis
Electrolyte
Notes: Todd

## Slide 10
Nanoparticle Synthesis
Sodium Carbonate
CuCl2 + 2NaOH- → CuOH2 + 2NaCl
CuCl2 + Na2CO3 → CuCO3 + 2NaCl
CuCl2 + 2NaI → CuI2 + 2NaCl
Sodium Iodide
Sodium Hydroxide
-No aggregation
-Small size
-Stable peak -Excellent TEM imaging
-Aggregation
-Small size at high PVA
-Unstable peak
-Poor TEM imaging
-Aggregation
-Small size at high PVA
-Unstable peak -Poor TEM imaging
Notes: Todd

## Slide 11
Research Design
  Analytical Design
Characterization
-HDD
-UV-Vis
-TEM/EDX
  Synthesis
  -Carbonate
  -Iodine
  -Hydroxide
Notes: Todd

## Slide 12
Nanoparticle Characterization
HDD (Hydrodynamic Diameter)
UV-Visible Spectroscopy
TEM Imaging & EDX
Size (nm)
0% PVA-1% PVA
Absorbance of light
Wavelengths & Intensity
Visualize particles
Element recognition
Notes: Todd
Morphology (size, shape, and dispersity)
Confirms elemental Copper spectrum

## Slide 13
HDD Results
Chart: Cu/PVA Nanocomposite Particle Diameter
| 0 | 0.05 | 0.1 | 0.2 | 0.5 | 1
 | 5000 | 6200 | 75 | 520 | 505 | 840
PVA (%) | Size (nm)
0 | 5000
0.05 | 6200
0.1 | 75
0.2 | 520
0.5 | 505
1 | 840
Notes: Kim
Hydrodynamic diameter (PVA)

## Slide 14
UV-Vis Results
Wavelength (nm)
Absorbance (AU)
Absorbance and Wavelengths of Cu/PVA Nanocomposites With Varying Amounts of PVA
Copper Nanoparticles
~570 nm
Ionic Copper
~800 nm
PVA
~276nm
Notes: Kim
Checked using TEM

## Slide 15
0.1 PVA
TEM Results
Cluster of nanoparticles
Polymer
Polymer
0.2 PVA
0.5 PVA
100K X
100K X
100K X
Notes: Todd
5 nm
Sphere
Mono = same size
Poly = different size

## Slide 16
EDX Results
Copper Carbonate 0.2 PVA:
Elements Present in Sample
Copper Hydroxide 0.2 PVA:
Elements Present in Sample
Copper Iodide 0.1 PVA:
Elements Present in Sample
Notes: Todd

## Slide 17
Research Design
  Analytical Design
Characterization
-HDD
-UV-Vis
-TEM/EDX
-Metal Analysis
Impact of Environmental Factors
pH, ionic strength, humic acid
  Synthesis
  -Carbonate
  -Iodine
  -Hydroxide
Degradation of Organic Pollutants
Notes: Kim

## Slide 18
Environmental Factors
Ionic strength (1, 10, 100 mM)
Eletrolyte valence (monovalent & divalent)
Humic Acid (0, 5, 20 mg/L)
pH (5, 7, 9)
Notes: Kim
Size (HDD)

## Slide 19
Impact of Environmental Factors
Notes: Kim

## Slide 20
Methylene Blue Degradation
Methylene blue (50 µM)
Cu/PVA (62.5 – 500 mg/L)
UV Light, Room, Dark
UV-Vis Spectroscopy
To what extent will Cu/PVA nanocomposites degrade organic pollutants?
Notes: Todd
2 ml filtered sample at 0 30 60 120
Model of organic pollutants
Decrease in absorbance = degredation

## Slide 21
Degradation Results
500 mg/L most successful
Catalytic, not photocatalytic
Degradation rate not significant
Notes: Todd

## Slide 22
Research Conclusions
Goal:
Synthesize environmentally benign Cu/PVA nanocomposites
Conclusions:
Stability increases with PVA polymer
TEM images show nanoparticles with sizes less than 5 nm
The EDX provided a confirmation that Cu was present in the Cu-based nanoparticles
Stable suspensions at pH 7 and above in all environmental conditions
Potential application to degrade organic pollutants in high Cu concentrations
Notes: Kim

## Slide 23
Todd Hamilton: CBL Unit
Topic: Water Filtration
Essential Question: How can water be filtered using rocks, minerals, and soil?
Challenge: Create a water filtration system using only materials found in nature to survive dehydration while stranded in the wild.
Notes: Todd

## Slide 24
Kim Lykens: CBL Unit
How does metal in our water affect human health?
How can we prevent metals from leaching into water?
How do the metals in drinking water in Dayton affect our quality of life?
EDP
Essential
Question
Reducing Cu Leaching into groundwater
Big Idea
Water Contamination
Notes: Kim

## Slide 25
Borm, P., Robbins, D., Haubold, S., Kuhlbusch, T., Fissan, H., Donaldson, K., Schins, R., Stone, V., Kreyling, W., Lademann, J., Krutmann, J., Warheit, D., Oberdorster, E., 2006. The potential risks of nanoparticles: a review carried out for ECETOC. Particle Fibre Toxicol. 3, 11.
Fritz, G., Volker, S., Willenbacher, N., & Wagner, N.J. (2002). Electrostatic stabilization of colloidal dispersions. Langmur, 18(16, 6381-6390.
Patachia S. (2003). Blends based on poly (vinyl alcohol) and the products based on this polymer. In Handbook of Polymer Blends and Composites, Vasile C., Kulshreshtha A.K. (Eds.), RAPRA Technology Ltd, Shrewsbury, UK, 285-364.
Ramesh, C., Hariprasad, M., Ragunathan, V., and Jayakumar, N. (2012). “A novel route for synthesis and characterization of green Cu2O/PVA nano composites.” European Journal of Applied Engineering and Scientific Research, 1(4), 201-206.
Bibliography
Notes: Both

## Slide 26: Questions?
Notes: Both