## Slide 1: Improvement of Lithium- Sulfur Fiber (Li-S) Batteries
Faculty Advisors: Dr. Shanov and Dr. Alvarez
GRA: Yanbo Fang
Presenters: Megan Stafford and Aaron Debbink
RET is funded by the National Science Foundation, grant EEC #17110826

## Slide 2: TABLE OF CONTENTS
Why Advanced Batteries
Introduction of Lab Goals
Abstract
Background Literature Review
RET Goals and Objectives
Research Training Received
Research Results
Unit Topic, Essential Question and Challenge
Notes: Megan

## Slide 3
6.58
2020
3.64
2018
“Forecast on connected devices per person worldwide 2003-2020 | Statistic.” (2016). Statista, PwC, <https://www.statista.com/statistics/678739/forecast-on-connected-devices-per-person/> (Jul. 5, 2018).
for each Person Worldwide
2010
1.84
Connected Devices
Notes: Megan
Emphasize wearable to lead into fiber battery
3.64 presently: https://blog.globalwebindex.com/chart-of-the-day/digital-consumers-own-3-64-connected-devices/

## Slide 4: LAB GOALS
Develop sensors using carbon nanostructures
Develop and test energy-dense supercapacitors using carbon nanostructures
Develop and test energy-dense batteries using carbon nanostructures
Notes: Aaron

## Slide 5: ABSTRACT
Interest in the development of energy-dense fiber batteries.
Lithium-sulfur batteries offer a high theoretical energy density but have major limitations.
Develop a highly conductive, mechanically strong cathode which can be used in a fiber battery.
Notes: Aaron
1) (RET) Higher conductivity (resistivity) and mechanically stronger (tensile tester) substrate for the S-CNT cathode to be used for the Li-S fiber battery.
  S-CNT allows the battery to have a high capacity
  Densified CNT gives the cathode a higher conductivity and mechanical strength.
2) (Maybe) Test effect of gel electrolyte and change components of gel electrolyte for better ion transfer rates and faster reaction kinetics. This must be addressed since previous charging at higher currents…
>> to limit polysuflide shuttling and faster...

## Slide 6: FIBER BATTERY
Notes: Megan
Introduction to what a fiber battery is with need to be flexible with emphasis on wearable technology

## Slide 7: LITHIUM SULFUR BATTERIES
Benefits
High theoretical capacity to store electric charge (1675 mA h g-1)
One of the most abundant elements, economical
Environmentally friendly
Chung, S., Manthiram, A., Zu, C. (2015). “Lithium-Sulfur Batteries: Progress and Prospects.” Advanced Materials, 27, 1980-2006
Limitations
Low conductivity
Low tensile strength
Fragile
Notes: Megan
1) (RET) Higher conductivity (resistivity) and mechanically stronger (tensile tester) substrate for the S-CNT cathode to be used for the Li-S fiber battery.
  S-CNT allows the battery to have a high capacity
  Densified CNT gives the cathode a higher conductivity and mechanical strength.
2) (Maybe) Test effect of gel electrolyte and change components of gel electrolyte for better ion transfer rates and faster reaction kinetics. This must be addressed since previous charging at higher currents…
>> to limit polysuflide shuttling and faster...

## Slide 8: CATHODE DESIGN
= Sulfur clusters/agglomerates
= Carbon Nanotube
Notes: Aaron
Use manipulative: sulfur low conductivity and is brittle and must be able to withstand deformations. Sulfur needs encapsulated inside of CNT (explain a CNT).

## Slide 9
Schematic illustration of the fabrication of a CNT-sulfur composite battery
Carbon Nanotube Array
Fiber CNT Spinning
Sulfur Melting Infiltration Synthesis
CNT + S
@ 155℃
O2 Plasma Functionalization
O
2
He
Coin Cell Assembly
BATTERY ASSEMBLY
Notes: Aaron
think about who our audience is: non-scientists

## Slide 10: GOALS AND OBJECTIVES
Create a hybrid carbon nanotube (CNT) thread using sulfur-loaded CNT and a densified CNT to increase conductivity and tensile strength.
Use the hybrid thread as the cathode in the assembly of a lithium sulfur fiber battery.
Notes: Megan

## Slide 11
Lab Training:
Equipment and Characterization
RESEARCH TIMELINE
Hybrid thread assembly
Begin research paper
04
Lab Training:
Construct cathode and coin cells
03
02
Literature
Review
01
05
Analyze battery results
Assemble additional coin cell batteries for testing
06
Tensile strength testing
Finish research paper
Notes: Megan

## Slide 12
Sulfur CNT Thread
Hybrid CNT Thread
Densified CNT Thread
HYBRID CATHODE
Notes: Aaron

## Slide 13: RESEARCH TRAINING ASSEMBLY
RET Teacher preparing CNT thread for Oxygen Plasma Functionalization
Autoclave containing CNT thread and Sulfur
Winding Hybrid CNT Cathode
CNT Array spun into CNT thread
Notes: Aaron
Change CNT to hydrophilic to help ease Sulfur loading
Introduce defects to the CNT to help Sulfur load to the outside and inside of the CNT

## Slide 14: RESEARCH TRAINING CHARACTERIZATION
RET Teachers viewing CNT thread on SEM
Nyquist Plot of Impedance
Coin Cell Testing with E.I.S.
SEM showing hybrid CNT thread
500x
R = ?x
Notes: Megan
Change CNT to hydrophilic to help ease Sulfur loading
Introduce defects to the CNT to help Sulfur load to the outside and inside of the CNT
Uses different charging frequencies to measure electrochemical cell properties: resistance and ion conductivity.

## Slide 15: RESEARCH RESULTS Sulfur- Loaded CNT Threads
57.4% Sulfur
63.4% Sulfur
66.5% Sulfur
Diameter: ~85 μm
Diameter: ~86 μm
Diameter: ~107 μm
Notes: Aaron

## Slide 16: HYBRID THREAD ASSEMBLY
Hybrid CNT threads.
a) pulling rate of 1.6 mm/s and a spinning rate of 1,060rpm.
b) pulling rate of 1.9 mm/s and a spinning rate of 1,310 rpm.
c)pulling rate of 1.2 mm/s and a spinning rate of 1,310 rpm
S-CNT
D-CNT
a)
b)
c)
Notes: Megan
Assembly of Hybrid Cathode: Attempted different spinning techniques by varying linear feed and rotation rates.

## Slide 17: Tensile Testing Results
densified= 1.4x stronger
densified= 5x more flexible
Notes: Aaron
Uses different charging frequencies to measure electrochemical cell properties: resistance and ion conductivity.

## Slide 18: CONDUCTIVITY TESTING RESULTS
Hybrid CNT thread
ZReal = 32.8 ohms
ZReal = 989 ohms
Single CNT thread
Zreal (ohms)
Zimaginary (ohms)
Notes: Megan

## Slide 19: Battery Cycling Results
Overall higher capacity
Notes: Aaron
Uses different charging frequencies to measure electrochemical cell properties: resistance and ion conductivity.

## Slide 20: MEGAN’S UNIT ALGEBRA 2 BIG IDEA DESIGN CHALLENGE ESSENTIAL QUESTION
Use MacBooks to analyze battery consumption and graphically interpret data to create a set of criteria for ideal battery consumption.
Criteria for Optimal Battery Usage
How can we use math to illustrate the criteria for optimal battery use?
1
2
3

## Slide 21: AARON’S UNIT AP PHYSICS 2 BIG IDEA DESIGN CHALLENGE ESSENTIAL QUESTION EXTENSION PROJECT
Design a process to test individual lithium-ion cells to determine which cells have more usable life and which cells will need to be recycled.
Lithium-ion Batteries and Energy Storage
What can be done with all the rechargeable batteries which appear to have no usable life?
1
2
3
4
Build a small Li-ion battery back to charge a cell phone.
Notes: Aaron

## Slide 22: QUESTIONS?
RET is funded by the National Science Foundation, grant EEC #17110826
Notes: Aaron